## Slide 1
RFQ
SRF Linac
Injector
Li Loop
Beam Dump
Post Irradiation Examination
Nuclear HVAC
Industrial HVAC
Electric Power Supply
Test Cell
RF Modules
Access Cell
PIE Detritiation Process
Wally
IFMIF
the neutron source for the Fusion Program
IAEA Fusion Energy Conference
Kyoto
October 2016
J. Knaster, R. Heidinger and S. O’hira
on behalf of IFMIF/EVEDA team
0
10m

## Slide 2
The first wall
of the reactor vessel shall
absorb 14.1 MeV neutrons
product of DT reactions
ITER first wall will present
3 < dpa at the end of its operational life
In a Fusion power plant
~15 dpa per year of operation
Two transmutation reactions become critical
56Fe(n,α)53Cr
and
56Fe(n, p)56Mn
with n threshold energies at 2.9 and 0.9 MeV
Nuclear Fusion
the potential energy solution for humankind
Blanket
Divertor
ITER
Where is
Wally?

## Slide 3
Structural Fusion materials are to withstand the combination of
High fluxes (and fluences)
1018 n/m2s
Cyclic stresses
Δσ > 100 MPa
(Maxwell stresses)
Thermal loads
>10 MW/m2
(critical in W based divertor)
He&H generation
~12 appm He/dpa
Neither fission reactors (0.3 He/dpa) nor spallation sources (>50 He/dpa)
give needed answers
Unique features of fusion materials

## Slide 4
Fission reactors n average energy <2 MeV
Spallation sources present a wide spectrum
with tails reaching impacting particle energy
~20 n per reaction
and are pulsed
No efficient
p+ or α-particle generation
Available neutron sources
Watt
Distribution
(fission n spectrum)
Fission
Spallation

## Slide 5
A 2 GW DEMO will reach ITER’s expected degradation damage
in a couple of months operating at full power
dpa
Known degradation
under fission neutrons
Guess of
Fusion neutrons
From ions impl. & spallation
fusion oriented experiments
30
Expected behavior
tbc in a Li(d,xn)
Radiation-induced
degradation
We need data
from all possible sources
from fission reactors
from spallation sources
from ion implantation
from a 14 MeV neutron source
Uncertainties (many) present
ITER
3
~ 2 years
DEMO Operation
Fusion relevant neutron sources are indispensable
Thanks
to Tanigawa-san

## Slide 6
A worldwide R&D and design work
has continuously been in place since the ‘70s
FMIT (80s in the US) – ESNIT (90s in Japan)
IFMIF for last 20 years
Initially as a US, RF, JP & EU collaboration up to 2007
P. Grand et al., An intense Li(d,n) neutron radiation test facility for controlled thermonuclear reactor materials testing, Nuclear Technology, Vol 29, p. 327 (1976)
Lithium
loop
Li(d,xn)
Neutron
En ~ 0.4Ed
Accelerator Facility
Target Facility
Test
Facility
Four decades of work towards a Li(d,xn) facility
R. Serber, The Production of High Energy Neutrons by Stripping, Phys. Rev. Vol. 72, No 1 (1947)

## Slide 7
E.W. Pottmeyer Jr., The Fusion Material Irradiation Facility at Handford, Journal of Nuclear Materials 85 & 86 (1979) 463-465
J. Knaster et al, The accomplishment of the Engineering Design Activities of IFMIF/EVEDA: The European–Japanese project towards a Li(d,xn) fusion relevant neutron source, Nuclear Fusion 55 (2015) 086003
Four decades of work towards a Li(d,xn) facility
FMIT
IFMIF

## Slide 8
IFMIF/EVEDA
IFMIF
International Fusion Materials Irradiation Facility
EVEDA
Engineering Validation & Engineering Design Activities
…to produce an integrated engineering design of IFMIF and the data necessary for future decisions on the construction, operation, exploitation and decommissioning of IFMIF, and to validate continuous and stable operation of each IFMIF subsystem
Signed in February 2007
Framed by the Broader Approach Agreement
Tokyo University
Kyushu University
Osaka University
Nagoya University
Tohoku University
Hachinohe Institute of Technology
Hachinohe National College of technology

## Slide 9
IFERC
DEMO
The Broader Approach Agreement
since 2007
JT60
JT-60SA
IFMIF/EVEDA

## Slide 10
IFMIF concept
Availability of facility >70%
A flux of neutrons of ~1018 m-2s-1
is generated in the forward direction
with a broad peak at
14 MeV
Two concurrent
125 mA CW deuterons beam
at 40 MeV
impact with
a beam footprint of 200 x 50 mm2
on a liquid Li screen
flowing at 15 m/s
and irradiate three regions
>20 dpa/y in 0.5 liters
>1 dpa/y in 6 liters
<1 dpa/y in 8 liters
14 MeV
~40 MeV
Notes: IFMIF will generate a neutron flux with a broad peak at 14 MeV by Li(d,xn) nuclear reactions thanks to two parallel deuteron accelerators colliding in a liquid Li screen with a footprint of 20 cm x 5 cm. The energy of the beam (40 MeV) and the current of the parallel accelerators (2 x 125 mA) have been tuned to maximize the neutrons flux (1018 m-2s-1) to get irradiation conditions comparable to those in the first wall of a fusion reactor in a volume of 0.5 l that will house around small 1000 specimens

## Slide 11
Engineering Design Activities – EDA phase
Validation Activities – EVA phase
EVEDA = EDA + EVA Phases
Successfully delivered on schedule
J. Knaster et al., IFMIF: overview of the validation activities, Nuclear Fusion 53 (2013) 116001
0
10m
RFQ
SRF Linac
Injector
Li Loop
Beam Dump
Post Irradiation Examination
Nuclear HVAC
Industrial HVAC
Electric Power Supply
Test Cell
RF Modules
Access Cell
PIE Detritiation Process
Human
J. Knaster et al, The accomplishment of the Engineering Design Activities of IFMIF/EVEDA: The European–Japanese project towards a Li(d,xn) fusion relevant neutron source, Nuclear Fusion 55 (2015) 086003

## Slide 12
It includes
>100 technical reports
interfaces with thorough 3D models, licensing scenarios,
RAMI analysis, nuclear safety studies, beam dynamics,
35 Detail Design Description documents of all sub-systems
and cost&schedule
Engineering Design Activities (EDA) Phase

## Slide 13
Deuteron beams 2 x 125 mA in CW
40 MeV energy
2 x 5 MW beam power
J. WEI et al., The very high intensity future, IPAC 2014, Dresde
EVA Phase – Accelerator Facility

## Slide 14
L
M
H
D+ Accelerator incident current 125 mA
100 keV 5 MeV 9 14.5 26 40 MeV
RFQ
Ion
source
LEBT
MEBT
HEBT
Superconducting
cavities
RF Power
EVA Phase – Target Facility
Lithium jet
at 250 C
Flow speed 15 m/s
Thickness 25±1 mm

## Slide 15
EVA Phase – Test facility
L
M
H
Test Cell
100 keV 5 MeV 9 14.5 26 40 MeV
RFQ
Ion
source
LEBT
MEBT
HEBT
Superconducting
cavities
RF Power
HFTM
20 dpa/y in 500 cm3
12 x 80 small specimens
independently cooled
within +/3% T

## Slide 16
The validation activities covered
a very wide range
There is no time to cover the full scope
in this talk
I will focus on identifying those historical main technological challenges
and explain how EVEDA has addressed them
J. Knaster et al., IFMIF: overview of the validation activities, Nuclear Fusion 53 (2013) 116001

## Slide 17
1st concern: D+ accelerator of 125 mA CW at 40 MeV
D+ prototype accelerator of 125 mA CW at 9 MeV in Rokkasho
2nd concern: Stable flow of lithium at required performance
Full scale prototype of Li facility in Oarai
3rd concern: Irradiated capsules allowing independent cooling
High Flux Test Module prototype in KIT
4th concern: Small Specimens Test Techniques
Shape validation for pending specimens in Japanese Univers.
5th concern: 2 x 5 MW beam vs target interaction
Suitable concave backplate design assessed
Five major historical technical concerns addressed
in IFMIF/EVEDA
Rokkasho
Oarai
Karlsruhe

## Slide 18
1st concern: D+ accelerator of 125 mA CW
IFMIF
LIPAc
Small in size but
big in performance

## Slide 19
Injector + LEBT
CEA Saclay
RFQ
INFN Legnaro
QST
MEBT
CIEMAT Madrid
SRF Linac
CEA Saclay
CIEMAT Madrid
HEBT
CIEMAT Madrid
BD
CIEMAT Madrid
Diagnostics
CEA Saclay
CIEMAT Madrid
RF Power
CIEMAT Madrid
CEA Saclay
SCK Mol
36 m
Cryoplant
CEA Saclay
Building
Auxiliary System
Control system
Installation
QST
Equipment designed
and constructed in Europe
Installed and commissioned in Rokkasho
★
Rokkasho
EVA Phase – Accelerator Facility

## Slide 20
LIPAc is very ambitious
World’s highest current linac
World’s top H+&D+ injector performance
World’s longest RFQ
World’s record of light hadrons current through SC cavities
World’s highest beam perveance
P. Cara et al., The Linear IFMIF Prototype Accelerator (LIPAc) design development under the European-Japanese collaboration, IPAC 2106 - Busan
1st concern: D+ accelerator of 125 mA CW
The accelerator
of records
MPT/P5-13
A. Kasugai et al., Progress on the Development of Linear IFMIF Prototype Accelerator and the Beam Commissioning

## Slide 21
D-plate
RF Power
9.8 m long RFQ
during bead pulling exercise
May 2016
Ion source + LEBT
Rokkasho Fusion Institute
RFQ RF Power
MPT/P5-13
A. Kasugai et al., Progress on the Development of Linear IFMIF Prototype Accelerator and the Beam Commissioning
Diagnostic Plate
Are we technologically ready for such accelerator?

## Slide 22
The 1st attempt to run a RFQ in CW was in Los Alamos (LANL)
for FMIT accelerator validation exercise
The ‘beam halo’ was discovered the rough way
Beam quality injected in RFQ was poor
ECR approach was technologically validated for H+ in Chalk River
LANL successfully operated LEDA
100 mA in CW at 6.7 MeV
with a dual electrodes capacitive/inductive part cooling RFQ tuning
and unraveled beam halo physics the following years
Alvarez type accelerating structure (DTL)
for beam energies within 0.2<β<0.6
is a difficult challenge for high currents in CW
the feasibility of superconducting resonators for low-β
was demonstrated in LANL in 2002
Operation of superconducting HWR cavities in CW
SARAF has operated 176 MHz HWR cavities in CW in 2010
Evolution of accelerators technology since FMIT
LIPAc implements best possible technologies
M. Kelly, Superconducting Radio-Frequency Cavities for Low-Beta Particle Accelerators, Reviews of Accelerator Science and Technology 5:185 (2012)
T. Taylor and J.S.C. Wills, A high-current low-emittance dc ECR proton source, Nucl. Instr. Meth. Phys. Res. A309, (1991)
C.K. Allen et al., Beam-Halo Measurements in High-Current Proton Beams, Phys. Rev. Lett. 89, Number 21, 18 Nov. 2002
L.M. Young et al., High power operations of LEDA, LINAC 2000, Monterey
W.D. Cornelius, CW operation of the FMIT RFQ accelerator, Nucl. Instr. Meth. Phys. Res. B10/l1 (1985) 859-863
J. Knaster and Y. Okumura, Accelerators for fusion materials testing, Reviews of Accelerator Science and Technology 8, 115142 (2015)
D. Berkovits et al., Operational experience and Future goals of the SARAF proton/deuteron linac, LINAC 2012, Tel-Aviv
80s
90s
1999
2001
2001
2010
T. Tajima, et al., Evaluation and Testing of a Low-β Spoke Resonator, PAC 2001, Chicago

## Slide 23
The mandate was challenging
the demonstration
of the flow operational conditions of IFMIF lithium target
Lithium temperature at 250 °C
Flow speed at 15 m/s
Stable flow with +/- 1 mm amplitude
10-3 Pa on free surface
Long term operation stability
Free surface interferometry diagnostics
Feasibility of Impurities in lithium <10 ppm
2nd concern: Stable flow of lithium at required performance
Kondo, H. et al. Validation of IFMIF liquid Li target for IFMIF/EVEDA Project, Fusion Eng. Des. 9697, 117122 (2015)
Operated until October 2014

## Slide 24
The result of 25 days
continuous operation (24 h/day)
2nd concern: Stable flow of lithium at required performance
MPT/P5-11
H. Kondo et al.,
Validation of Liquid Lithium Target Stability for Intense Neutron Source
Long term flow stability demonstrated
MPT/P5-41
F. Arbeiter et al.,
The Accomplishments of Lithium Target and Test Facility Validation Activities in the IFMIF/EVEDA Phase

## Slide 25
Arbeiter, F. et al. Design description and validation results for the IFMIF HighFlux Test Module as outcome of the EVEDA phase, Nuclear Materials and Energy (2016)
3th concern: Irradiated capsules allowing independent cooling
Target T uniformity of specimens demonstrated
HFTM-Double Compartment
HELOKA
MPT/P5-41
F. Arbeiter et al.,
The Accomplishments of Lithium Target and Test Facility Validation Activities in the IFMIF/EVEDA Phase

## Slide 26
Small specimens
are neither exclusive of fusion
nor a new technology
Under EVEDA intense work has been developed on
Fatigue
Fracture toughness
Crack growth rate
4th concern: Small Specimens Test Techniques

## Slide 27
12 capsules within beam footprint
x2 sets of 40-45 spec/capsule
within 3% ΔT/capsule
80-90 specimens/capsule
Specimen filling in hot cell
4th concern: Small Specimens Test Techniques
Thermalized with NaK
8 compartment
4 central directly irradiated

## Slide 28
Fatigue matches standard specimens
Master Curve for ferritic steels under
ASTM E1921 did not work
an adaptation is being studied
4th concern: Small Specimens Test Techniques
MPT/P5-25
E. Wakai et al., Small Specimen Test Technology Develop. towards Design of Fusion DEMO Reactors and Future Direction Plan
IAEA’s Coordinated Research Project launched
‘Towards standardization of SSTT for Fusion applications’
Notes: The purpose of the Creep Fatigue Test Module (CFTM) in IFMIF is to perform creep fatigue experiments under intense neutron irradiation. A CFTM prototype has been built and extensively tested at Villigen. The final CFTM will consist of three parallel load controlled single testing machines (STM), mounted on a frame. The three testing machines will operate independently with +/-12.5 kN load with controlled speed ranging between 1 μm/s and 80 μm/s. The complete CFTM will be installed in the medium flux area of IFMIF test cell and will be exposed to intense radiation fields, including both neutron and gamma fields. The heat absorbed by the different parts of the module will be extracted by means of a helium gas (coolant) passing through independent cooling channels.
Due to the limited irradiation volume available in the test modules, small specimen test technique (SSTT) is being developed under IFMIF/EVEDA frame by various Japanese universities (College of Hachinohe, Kyoto University and Tohoku University) and institutions (NIFS) under the coordination of JAEA . The understanding fracture mechanics of irradiated specimens as well as fatigue behavior in the irradiated materials of the first wall in the fusion reactor vessel is essential.
Two types of fatigue specimens were tested with a perfect match for the round bar type in the range of interest . Further tests are needed to understand a slight deviation from the expected hysteresis behaviour.
Transition fracture toughness has been measured with ¼CT-specimens aiming at the definition of Master Curve (MC) following ASTM E1921 ‘Determination of Reference Temperature, To, for Ferritic Steels in the Transition Range’. Results indicate that the correlation developed for ferritic steels cannot be exactly applied. A new correlation has been proposed, but further tests are needed to statistically secure it.
It is to be noted that Charpy tests for miniaturized specimens is already covered by ASTM E1253 ‘Reconstitution of Irradiated Charpy-Sized Specimens’.
The crack growth rate through environmental assisted cracking and stress corrosion cracking has been assessed for RAFM by Hachinohe College with no significant difference observed with the data accumulated with austenitic steels.

## Slide 29
Design of the Li target implements
the lessons learnt
throughout 30 years of studies
Bragg’s peak in Li of 40 MeV at 19 mm
25 mm thick screen +/-1 mm perturbations
Power density of 1 GW/m2 (beam footprint maximized)
~x10 lower than FMIT
Concave back plate leads to kPa centrifugal pressures
Maximum pressure waves amplitudes of 32 Pa
15 m/s liquid Li speed evacuate the beam power
Vmax = 0.5 m/s of wave pressure prevents resonances
5th concern: Beam – Li target interaction
Temperature profile along channel[K]
J. Knaster et al., Assessment of the beam-target interaction of IFMIF: state of the art, Fusion Engineering and Design 89 (2014) 1709–1716
Italics fonts
results achieved
Y. Momozaki et al., Proton beam-on-liquid lithium stripper film experiment,
J. Radioanal Nucl. Chem. (2015)

## Slide 30
Possibly not
one only accelerator suffices
to cope with present DEMO expected performance
A sensitivity analysis with involved parameters
has been carried out
F. Mota et al., Sensitivity of IFMIF-DONES irradiation characteristics to different design parameters, Nuclear Fusion (2016)
Do we need IFMIF?
>20 dpa/fpy

## Slide 31
The EDA Phase was successfully accomplished on schedule
IFMIF nominal flow operational conditions of liquid lithium
have been validated
IFMIF HFTM specs
have been validated
LIPAc commissioning is advancing in Rokkasho
125 mA in CW 40 MeV deuteron accelerator
is nowadays at hand of technology
The on-going success of IFMIF/EVEDA
allows us to expect counting next decade
with a Li(d,xn) fusion relevant neutron source
adapted to fusion community needs
Conclusions
for a marginal cost of a fusion reactor

## Slide 32
Thanks to the EU-JA IFMIF team
(and all people involved in former phases/projects)
for their resilient enthusiasm
crucial for the present success of the program