## Slide 1: Targets, at the Center of ICF Experiments and Research
Presented at
41ST ANNUAL FUSION POWER ASSOCIATES MEETING
Virtual/Remote Meeting
By
Mike Farrell
Inertial Fusion Technology Division
December 16-17, 2020
Be
CH
HDC
W/Be
Cr/W
Be

## Slide 2: Advances in ICF Drivers, Simulations, & Diagnostics Need to be Matched by Advances in Targets Manufacture and Metrology
~15,000 targets for experiments at
“Focus” is on the target
Recent advances for indirect drive
The increasingly complex direct drive capsule
Applying knowhow to MagLIF targets
Additive manufacturing for smaller facilities
Rep-rated research efforts

## Slide 3: After Recent Facility and Diagnostic Improvements Focus is Now on the Target
Instability seeds & growth
Edwards (LLNL): JASON Summer talk
Shell spherical variations
Casey (LLNL): APS talk
Engineered features
LANL: Invited APS talk
2020 JASON & APS DPP talks spoke to observed and simulated target related concerns

## Slide 4: Target Metrology is Providing Increasingly Detailed Information Shell-by-Shell (Thereby informing both the simulations as well as the fabrication process)
Defect specific
Location within shell wall
Multiple Perspectives
Volume, Type, Composition
Local Location
Global Location
Shell Wall
# of Defects
3D position

## Slide 5: Assembling a Tiny Three Dimensional Puzzle
Spherical (3D) TARGET DATA is increasingly important to physics understanding
Correlating data with fiducials enables known positioning of shell imperfections
The Objective
The Metrology
Known orientation at shot time
Spherical figure
Surface roughness
Thickness variation
Wall homogeneity
  Composition
  Voids
  Inclusions

## Slide 6: Research into Amorphous Ablator Materials is occurring at GA & LLNL (Eliminate crystalline microstructure inherent High Density Carbon & Be shells)
Commercially
available stationary
coating
Rotating Hollow Cathode
coating apparatus developed for shells
Proof-of-principle DLC/GDP shell
Prototype rotating apparatus constructed for DLC capsule fab
* Amorphous Carbon = sp3 phase = Diamond-Like-Carbon (DLC)
Planar DLC coating R&D
~undesirable quality, but demonstrates feasibility

## Slide 7: Other R&D Supporting Laser Indirect Drive
Additive Manufacturing for Selected Applications
Gradient Density
Metal Shells
CPC cone based
MeV & Gamma Backlighters
80X
2020
2019
Double Shell
cushion
(Improving feature size)
(Avoid glues by printing directly on objects)

## Slide 8: Using Larger, Shimmed and Soon-to-be Foam Covered Shells on NIF for Laser Direct Drive ICF and Neutron Sources
Scaling Shells
(Increased fuel load; Triple Shell scale)
Shell Thickness as a function of angle
~1-2 µm shimming the shell wall
(correcting sym. for NIF’s polar config.)
~0.9 mm
~5.0 mm
Exterior Conformal CH Foam Coating s (~15 mg/cc)
(Laser Imprint mitigation, Double Shell cushion)
~5.0 mm
~2.0 mm
Be
CH

## Slide 9: Applying Target Fab and Metrology Knowhow to Novel Cylindrical & Magnetized Liner Inertial Fusion (MagLIF) Targets
Improving Characterization
(Implosion Simulation & Stability)
Cryogenic Gas Cells
(Laser Pre-Heat)
Auto Magnetizing Target
(Improved B-field application)

## Slide 10: Increasing Use of Additively Manufactured Targets thru LaserNetUS (Enabling efficient design variation studies)
Focusing cone design variations
Microtubes: probing ion generation
Gradient Density Foam

## Slide 11: Developing a Facility to Support Control systems, Target fielding, and Diagnostics Research
GALADRIEL: GA LAboratory for Developing Rep-rated Instrumentation and Experiments with Lasers:
Anticipate future needs as HED research on rep-rate facilities (~0.1-10Hz)
Apply MFE knowhow: a) managing large data sets 2) active feedback control

## Slide 12: Developing Rep-rated Target System(s) Using GALADRIEL
Develop a liquid-leaf system to continuously create thin (<1𝛍m) films for proton generation
  Test designs for proton production
Demo robust ~MeV-proton generation
  Rep-rated spectroscopy, beam monitoring
  ~ps imaging of laser-liquid interaction
  Fast-analysis tools & feedback to laser system
Morrison et al, NJP 20 (2018)
Liquid-leaf Apparatus

## Slide 13: In Conclusion
Focus is turning to the target
Advances in drivers, simulations, and diagnostics need to be matched by advances in target fabrication, target metrology, and final assembly
A Partner in Science-Based Stockpile Stewardship and ICF Research for Three Decades
Be
CH
HDC
W/Be
Cr/W
Be