## Slide 1: Wetted Foam Targets for Inertial Fusion Power Plants
By
Neil Alexander
Director of Inertial Fusion Energy
Presented to
Fusion Power Associates
Washington DC,
December 19-20, 2023
Shell/capsule
Foam Shell
Hohlraum
Cone-in-shell

## Slide 2: Inertial fusion energy (IFE) power plant have a number key R&D needs
Injected targets
Tritium Processing
A proven, robust, (fabricable/affordable) target design
A long-life, affordable, high shot-rate, driver
Affordable, precise, mass-production of targets
A long-life, reliable target injector
Accurately hitting the targets on-the-fly
Survival of cryogenic target fuel to chamber heat flux
Debris/target waste removal/chamber reset strategy
Long-life final ‘optics’
An affordable target chamber survival strategy
Long-life blanket (tritium breeding and heat transport to power conversion)
Efficient tritium recovery and purification
Many items directly or indirectly involve the target
GA IFE Group’s Emphasis

## Slide 3: There are many potential IFE target types
New target designs may appear
Targets are <~~1cm in size
Each target design can be the core of an IFE plant
At a single driver facility many target designs can be tested
Several of the many IFE target types:
(a)
(b)
(c)
(e)
(h)
(f)
Solid DT in foam
Liquid DT in foam
Hollow cone
Hohlraum (High Z interior)
Cylindrical liner
(low Z)
Thin film windows and supports
Distributed radiators (metal foams)
Sealed capsule with IR reflective coat
Capsule with IR reflective coat
Solid pure DT layer
P2 Shield (High Z)
Capsule with IR reflective coat
(d)
(i)
(g)
Nano-wire forest
Pusher
Propellent
Tamper
Many target design utilize a spherical foam shell
“Wetted Foam”

## Slide 4: Inertial fusion energy (IFE) reactors use many targets
Goals for target factory mass production:
  Low cost targets
    Small fraction of energy value of target’s yield
    ~10’s cents laser and ion drive
    ~$2 pulse power
  High production rate
    ~1 to 10 Hz laser and ion drive,
    ~0.1 Hz pulse power drive
  High precision: ~10 µm
    Components and assembly
  Smooth surfaces: up to ~10’s to 100’s nm
Spherical shells, “cylinders”, cones, foams
Each target design has its own tolerances
The target needs to be fueled
  Cryogenic DT, usually “layered”
Shell/capsule
Foam Shell
Hohlraum
Cone-in-shell
Foam density for
“Wetted Foam” ~5 - 50mg/cc

## Slide 5: Studies have shown the feasibility of a cost-effective IFE target supply for energy
DT Vapor
Foam + DT
Thin (300-1200 Å)
High Z coating
~ 2.3 mm rad
1-10 m CH Overcoat
DT
Foam layer:
0.18 mm thickness Divinyl Benzene (DVB) or Resorcinol-Formaldehyde (RF)
Direct Drive Laser Fusion
Heavy Ion Fusion
Z-Pinch IFE (ZFE)
Laser Inertial Fusion Engine (LIFE)
Goodin, D.T., et al, “A cost-effective target supply for inertial fusion energy”, Nuclear Fusion 44 (2004).
~1 cm
If the selected process meets precision, targets should be affordable
% of Energy Value

## Slide 6: Our estimates for direct drive target production costs are encouraging
Chemical engineering approach to Target Fabrication Facility (TFF)
Costing is done for an “nth-of-a-kind” plant
    Major Parameters
    500,000 targets per day
    25% reject rate
    Installed capital of $97M
    Annual operating cost of $19M
    Cost per injected target estimated at 16.6 cents
Conceptual layout for NRL high gain target production
Nuclear Fusion, 44, (2004), 254-265
Full Presentation - HAPL April 4/5, 2002
(http://aries.ucsd.edu/HAPL/MEETINGS/0204-HAPL/program.html)
Each contactor:
ID 50cm x 50cm long
26 gallon (98 L)
~6% filled with targets
8 hours of targets at 6 Hz

## Slide 7: Polymer or foam capsules can be made at IFE rates by blowing “bubbles” in solution (aka micro-encapsulation)
Droplet generator produces at ~1Hz
Achieving high yield of centered capsules is the challenge
Polymer solution
Plain solution
SPEC
Non-Concentriicity, %
FOAM CAPSULES (100mg/cc) FROM HAPL ERA
Yield, %
Pumping solutions forms bubbles
Agitation and heat to center and cure bubble into capsules
DVB Foam capsules, 4.6 mm dia. X 180 µm wall
PAMS Capsules, 4.0 mm dia. x 35 µm wall
Solvent exchange and critical point drying
Today’s wetted foam target concepts will want lower foam density

## Slide 8: Mass production methods to over-coat foam shells were developed during the HAPL program
Seal large pores of foam with polyvinylphenol (PVP via interfacial condensation)
Reinforce with GDP layer (Glow Discharge Polymer)
Sputter coat an IR reflective layer on top (Au:Pd)
Overcoats
A) Interfacial reaction
B) GDP coating
C) Sputter coating of metal (Au/Pd)
Au/Pd alloys coated on shells for reflection of thermal heat load in reactor; hydrogen permeable
Interfacial Condensation
Solvent A with reactant C
Solvent B with reactant D
A & B immiscible, so C & D react at capsule surface to form layer
The rotary horizontal GDP coater scales to mass production – arbitrary length

## Slide 9: NEW – GA’s GACH foam chemistry adjusted for micro-encapsulation in droplet generators
Low density (2 – 200 mg/cc billets made), small pore size
Pure CH, no oxygen
Deuterated feed stock available for pure CD
Surface GACH micro-encapsulated bead, 25 mg/cc
Overcoats well (from foam billets)
First GACH foam compound droplets have been formed (25mg/cc nom.)

## Slide 10: GA has built its own, open architecture, 2 photon polymerization (2PP) additive manufacturing (AM) systems – Printing WF targets and foam inside of capsules demonstrated
2PP-AM graded density foam
Arbitrary structure printed inside of PAMS capsule
2PP printed shell with foam interior
2PP System at GA
Flexible output, sub-micron resolution
Determined structures, even foam structure
There are many strategies for increasing throughput (e.g. multiplexing 2PP laser; MHz)
Speed increase needed for IFE
Objective Lens
Objective Lens
Energy 1 Photon (1PP)
Conduction Band
Valence Band
e-
λ = 400nm
Conduction Band
Valence Band
e-
λ = 800 nm
800 nm
800 nm
Energy 2 Photon (2PP)
Polymerization Threshold α Ι
Polymerization Threshold α Ι2
0.5mm
Foam printed inside of GDP capsule still in resin

## Slide 11: Schemes to speed up additive manufacturing
Use area projection rather than scanning points voxels
  Use chemistry that turns into foam, instead of scanning foam struts
  4060 projections (1um) vs 2 billion voxel (1um)3 scan moves
Scan multiple capsules at once
  Each target is small, ~4mm
  Many will fit onto a single scanning stage
    662=4356 on (30 cm)2 stage
    24hr/4356= = ~20 sec
  Short pulse lasers have energy to support many simultaneous printing spots
    2000 demonstrated (W. Ouyang, Nature Comm. 2023)
Project cross-sections
Scan voxels
One pattern/laser in
Multiple patterns/lasers out

## Slide 12: GA developed a cryogenic fluidized bed for layering the DT/D2 solid fuel layers
Heat from beta decay (DT) or imposed IR D2 cause surface of DT/D2 to move until isothermal
  Thicker regions are hotter, higher vapor pressure, condense preferentially on thinner colder regions
In one target experiments, the capsule is placed in the center of a spherical cavity of a copper block to force a concentric spherical isotherm
In the cryogenic fluidized bed, the random spinning and circulation provides a time averaged spherical isotherm determined by the sphericity of the capsule
  Provide spinning is much faster than layering time constant (~1/2 hour for beta layering)
LAYERING
Fluidized Bed
Cryogenic Gas Flow
Frit
Layering cavity for one target
E-folding time of DT material migration is
Hs*ρs/qs = 26 minutes
qs volumetric heating DT 5.02e-2 W/cm3
Hs heat of sublimation of DT 1580 J/mol
ρs density of solid DT 5.03e-2 mol/cm3
11K bed Video, 1/17th normal speed, Empty capsules

## Slide 13: Wetted foam target concept - Filling via wicking into foam layer can be rapid
10 second fill time possible
Filling and layering occur simultaneously
Will lead to much lower tritium inventory than permeation filling
Foam layer
Fill Hole (Capillary)
Liquid DT
Capsule Wall
rcapillary := 0.005mm

## Slide 14: For LDD target, tritium inventory can be low for wetted foam target systems
Rough estimate, at least 1.8 gm Tritium needed for target systems
Does not include DT adsorbed on walls or permeated into reactor surfaces
Does not include reserve DT or reserve filled targets
For a DT mass multiply by 3/5 for tritium mass
Target DT mass 4.43 milligram (Olson et al PoP 2021 wetted foam target design; yield 62MJ)
Shot frequency 6 Hz (372MWthermal)
Fill and Layering Station
Liquid DT in condenser/HX/dispensing 1.14 gm T (1.9gm DT)
Equivalent to 1 m x 0.13” ID line
6 cups for filling
60 cups for wicking into foam capsule
59 cups for adjusting capsule fill
1 cup for target removal
Liquid DT in cups 0.62 gm T (1.03 gm DT)
Target to queue for injector
DT gas in
Cup
Capsule
R 3.343mm
Mid-point
chamber
Blanket
<<1 targets worth DT at shot time
? DT in blanket
Vacuum Pumps/disengagers
DT recovery System from Blanket (vacuum disengager)
Tritium Purification System
? DT in TPS
? DT
Fill and Layering Station
Queue for Injector
Target Injector
1 targets worth DT
3 targets worth DT
DT gas in Line 0.016 gm Tritium.
Line 25m x 0.13” ID;
T=300K; <P> = 0.61 atm

## Slide 15: Plenty of target R&D to do in IFE
Questions?
First GACH foam compound droplets have been formed (25mg/cc nom.)

## Slide 16: Outside-in construction would coat interior of capsules with foam using random rotation
Long spiral rotating curing tube would allow foam layer to coated inside of capsules in a continuous flow of capsules
Micro-encapsulate capsules
Laser drill hole in capsules
Fill capsules with foam forming solution
Rotating, varying pitch, spiral cure tube
Rotary slip joint